Abstract

Due to increasing the importance  which  was occurred in the last year for using composite materials in general and polymers in especial in different advanced industrial applications, so this research come to explaine and study the mechanical vibration damping  in polymeric composite materials which reinforced with fibers to know the importance of these fibers in vibration damping.

Epoxy and unsaturated polyester resin was used as a matrices for composite materials, with carbon, glass, and copper fibers as reinforcement materials with volume fraction (Vf =1%,2%,3%). Six types of composites were prepared:-

(1) Epoxy reinforced with continuous carbon fibers .

(2) Epoxy reinforced with short carbon fibers.

(3) Epoxy reinforced with continuous glass fibers.

(4) Epoxy reinforced with short glass fibers.

(5) Epoxy reinforced with continuous copper fibers.

(6) Epoxy reinforced with short copper fibers.

And another six types of composites were prepared :-

(1) Unsaturated polyester reinforced with continuous carbon fibers .

(2) Unsaturated polyester reinforced with short carbon fibers.

(3) Unsaturated polyester reinforced with continuous glass fibers.

(4) Unsaturated polyester reinforced with short glass fibers.

(5) Unsaturated polyester reinforced with continuous copper fibers.

(6) Unsaturated polyester reinforced with short copper fibers.

Research subject was implies studying some of mechanical  properties for composite materials in Natural conditions.

Mechanical properties that be studied were :- ( Vibration damping, and studying, deflection, stiffness, natural frequency, and damped period.

The research results showed that the values of (Stiffness, Natural Frequency, Vibration damping and Damped period) will increasing with the increase of the volume fraction of reinforcement materials used in this research, in the other hand the values for deflection will be decreeing with the increase of the volume fraction of the reinforcement materials used.